Study of Optical Properties of Non Stoichiometric Nickel Oxide

Lalit Kumar Bhataniya1, Aakanksha Chouhan1, Netram Kaurav2, a) and Paras Dubey1a)

1 Department of Physics, Institute of Sciences, SAGE University, Indore 452020

2Department of Physics, Government Holkar Science College,, Indore 452001, India

a) Corresponding author: paras_dubey74@yahoo.co.in, netramkaurav@yahoo.co.uk

Abstract. Non stoichiometric nickel oxide at different sintering temperatures upto 1100 °C were synthesis by thermal decomposition method. Structure of synthesis compound was characterization by X-ray diffraction method along with ritvield refinement. In UV-visible spectroscopy the band gap of the nonstoichiometric nickel oxide due to excitation of electrons can be obtained. The presence of Ni3+ ions in the oxide lattice shows charge transfer transition, with the consequent absorption in the visible region, which is mainly due to different ratio of Ni3+ and Ni2+ ions in the sample. These results were interpreted as the decomposition temperature increases, which heals the defects present in the non-stoichiometric nickel oxide and adjacent divalent nickel ions become Ni3+ due to charge transfer process caused by presence of nickel vacancy.